## Slide 1: Effect of evaporation reducers on concrete shrinkage
By: Armando De La Cruz
Faculty Mentor: Dr. Craig M. Newtson

## Slide 2: Purpose
Assess the effectiveness of the evaporation reducer, a.k.a Confilm®, in terms of its ability to minimize early-age
shrinkage in concrete.
Perform routine slump, compressive strength and flexural strength tests.
Gain a deeper understanding of concrete construction.
Be exposed to the engineering design of concrete mixtures.

## Slide 3: Description
Follow-up work to a study that evaluated early-age shrinkage in concrete cured by misting and wet curing.
Comparisons will be made to the original experimental results to assess the effectiveness Confilm®.
Types of tests performed
  Towels, no Confilm®
  No towels, no Confilm®
  Confilm® and towels
  Confilm® only

## Slide 4: Project Importance
Shrinkage cracks allow the infiltration of water, salts, and chemicals into concrete. This can lead into the following:
  Damage and corrosion of reinforcing steel
  Degradation of the concrete
  Decreased service life of the concrete
  Possible failure of a structure

## Slide 5: Methodology
Materials
There are five basic constituents in the concrete used:
  Cement -(Type I-II Portland Cement with a specific gravity of 3.15)
  Coarse Aggregate - (Specific Gravity of 2.55, absorption of 1.85 percent, and a 3/4 inch top size)
  Fine Aggregate -(Specific Gravity of 2.54, absorption of 1.14 percent)
  Water
  Air

## Slide 6
Example of ASTM C 143: slump test
Mixing Procedure
  Mixed according to ASTM C 192 (American Society for Testing and Materials)
  Materials had to be placed in two mixers: 53 % in the first, and 47% in the second
  The batch size for each of the tests was 3.50 ft3
  After mixing, ASTM C 143 slump test was performed to measure the workability of the concrete
Picture of mixers used

## Slide 7
Specimen Preparation
Specimens were produced by placing concrete into the following mold sizes and quantities:
  One 3ft x 1.5 ft x 0.5 ft (914.4x457.2x152.4 mm)wooden mold lined with two layers of plastic and talc in between the layers
  Three 4 x 8 inch (102x203.2 mm)cylinders
  Four 3 x 4 x 16 inch (76.2x102x406 mm) prisms

## Slide 9
Picture of molds
Picture of curing room used for cylinders

## Slide 10
Weighing the constituents.
Placing constituents into the mixers.

## Slide 11
Checking for clumping .
Placing cement into molds and specimen.

## Slide 12
Consolidating with electric vibrator.
Troweling surface for smooth finish.

## Slide 13
Placing frame used to hold LVDT’s.
Inserting hangers and LVDT’s.

## Slide 14
Data Acquisition
  Computer hardware used to collect the data was Super Logics WINview CP 32.
  Two Super Logic Analog Input Modules
  Two LVDT’s (linear variable differential transformer)
  Two thermocouples

## Slide 15
LVDT
Resistance spring
Hangers

## Slide 16
Strength Testing
  Compressive Strength Test (ASTM C 39)
  Modulus of Rupture Test (ASTM C 78)

## Slide 18: Results
Tests which used only Confilm® produced least amount of compressive strength.
(4454 psi)
Reduction of compressive strength by 19.3%.
Reduced tensile strength by 8.0%.
Test | MPa | (psi)
Dry Tests | 38.03 | 5516
Towel Tests | 32.93 | 4777
Confilm® Tests | 30.71 | 4454
Confilm®/Towel Tests | 32.38 | 4697
Average Compressive Strengths of Tests
Test | MPa | (psi)
Dry Tests | 4.48 | 650
Towel Tests | 3.95 | 573
Confilm® Tests | 4.11 | 597
Confilm®/Towel Tests | 4.57 | 663
Average Tensile Strengths of Tests

## Slide 19
Chart: Time (Hrs.)
Average Horizontal Strain Measurements
No curing aids-1000µε Wet towels only-200µε
Only Confilm®-147µε Towels and Confilm®-310µε

## Slide 20: Conclusion
When using Confilm, shrinkage decreased by 85.3%.
(1000µε to 147µε)
The use of confilm can be suitable in situations where the engineering properties of the concrete are not important (i.e. driveways, landscaping).
More experimentation is still required to establish a more accurate understanding of Confilm’s effect on concrete under varying outdoor conditions.

## Slide 21: Special Thanks:
New Mexico AMP
Dr. Craig M. Newtson
Christian Dominguez
National Science Foundation

## Slide 22: Questions?